Technical data sheet

CARBON ROVING HS230-3.5-4

HS230-3.5-4 carbon fiber is a high-strength, high-modulus fiber made from polyacrylonitrile-based (PAN) carbon fiber precursor through high-temperature carbonization. The product has characteristics such as uniform linear density, high tensile strength and modulus with low dispersion, good resin composite performance, minimal fuzziness, and good fiber spreading performance.

| Fiber specification | Product grade | Linear Density | Volume density | Tensile strength | Tensile modulus | Rupture elongation | Carbon content | Sizing |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | g/km | g/cm3 | GPa | GPa | % | % | % |
| HS230-3.5-4 | 12K | 800±20 | 1.78 | 3.5~<4.0 | ≥230 | ≥1.5 | ≥93 | 1.1 |
|  | 24K | 1600±40 | 1.78 | 3.5~<4.0 | ≥230 | ≥1.5 | ≥93 | 1.1 |
|  | 48K | 3700±100 | 1.78 | 3.5~<4.0 | ≥230 | ≥1.5 | ≥93 | 1.1 |

Standard packaging specifications:

12K/24K – 4kg/ bobbin  24kg/carton

48K – 4, 8, and 10kg/bobbin  24-30kg/carton

February 2024

Havel Composites CZ , s.r.o.,Svésedlice 67,Přáslavice,783 54

Phone: +420585129011

www.havel-composites.com, info@havel-composites.com