# Technical Datasheet: Glass braided sleeve

# Article code:	080.1445022300-S

technical details of material:

| Tensile strength | 3400 MPa |
| --- | --- |
| Tensile modules | 73000 MPa |
| Elongation | 4,5 % |
| Density | 2,6 g/cm³ |
| Material | Plastic sizing material (Glass) |

### technical details of article:

| Width, stretched | 25 mm |
| --- | --- |
| Wall thickness, | 0,25 mm |
| Threads | 144 |
| Filaments, stretched | 5,8 |
| Diameter | 20 – 95 mm |
| Weight per 100m | 4,415 kg |

We declare, that supply will be done as declared on confirmation.

All statements contain a tolerance of +/- 10 %.

SILTEX Flecht- und Isoliertechnologie Holzmüller GmbH & Co.KG  Palmstr. 27  D-84387 Julbach

Tel: +49-8571-922 970  Fax: +49-8571-6624  Internet: www.siltex.de  Email: siltex@siltex.de

HAVEL COMPOSITES CZ s.r.o. ,Svésedlice 67, 783 54 Přáslavice
                             tel.: +420 585 129 011  fax: +420 585 129 040
                             info@havel-composites.cz  www.havel-composites.com
                             IČ: 25907379 DIČ: CZ25907379